## Slide 1
Methods for Materials Diagnostics
Edmund (Edo) Dobročka
1975-1980 – Faculty of Mathematics and Physics, Charles University, Prague,
1980 -1991 – IEE SAS – X-ray topography, dislocations in Si substrates
and GaAs crystals
1991-2005 – Faculty of Mathematics and Physics, Comenius University, Bratislava,
lectures on X-ray diffraction methods, dislocations in solids
2005 - ?? – IEE SAS, X-ray diffracion, high power diffractometer
Bruker D8 DISCOVER with rotating anode
2004 -2015 – Faculty of Electrical Engineering, STU, Bratislava (part time job)
lectures on X-ray diffraction methods

## Slide 2
Introduction. Non-crystalline state. Hard-Sphere models, Random-Walk models,
Fractal models.
Crystalline state. Symmetry, symmetry operations, space lattice, unit cell, primitive
cell. Miller indices, crystallographic symbols. Crystallography in two dimensions.
Crystallography in three dimensions. Crystal systems, Bravais lattices, point groups,
space groups.
Symmetry and the properties of crystals. Neumann, Curie and Voigt principles.
Examples of structures. Imperfections in crystals and their experimental
observation. Point defects, dislocations, stacking faults.
Diffraction methods. Laue equations, reciprocal lattice, Ewald construction, Bragg
equation. Diffraction indices, atomic form factor, structure factor, intensity of
diffracted radiation.
Basic X-ray diffraction experiments, Debye-Scherrer method, Laue method, X-ray
diffractometry. Bragg-Brentano set-up, double axis and triple axis diffractometry.
Imaging methods, X-ray topography.
Methods for Materials Diagnostics

## Slide 3
Literature
Samuel M. Allen, Edwin L. Thomas: The Structure of Materials,
John Wiley & Sons, Inc., New York 1998, USA
J. C. Anderson, K. D., Leaver, R. D. Rawlings, J. M. Alexander:
Materials Science, Stanley Thornes (Publisher) Ltd, Cheltenham 1998, UK
J. F. Nye: Physical Properties of Crystals, Clarendon Press, Oxford 2006, UK
R. W. James: The optical Principles of Diffraction of X-Rays, Ox Bow Press,
Woodbridge, Connecticut 1948, USA
B. E. Warren: X-Ray Diffraction, Addison-Wesley, London 1969, UK
M. Birkholz: Thin Film Analysis by X-Ray Scattering, Wiley-VCH Verlag
GmbH & Co. KGaA, Weinheim 2006, Germany
V. Valvoda, M. Polcarová, P. Lukáč: Základy strukturní analýzy,
Karolinum, Praha 1992

## Slide 4
Introduction
Material Science and Engineering (MSE) – multidisciplinarity
MSE tetrahedron
Structure
Properties
Processing
Performance
ideal – perfect crystal
not always the best solution
role of lattice defects – important!!
point defects – microelectronics
dislocations – plasticity in metalurgy
New discipline – defect engineering!

## Slide 5
Defect engineering - example
Intrinsic gettering in Si wafers
growth of SiOx precipitates
denuded zone
dislocation loops punching
from SiOx precipitates
efficient sinks of
lifetime killers (Au, Pt, Ni,..)

## Slide 6
Structure – “definition”
quantitative description of the arrangements of the components that make up
the material on all relevant length scales
chemical composition
arrangement
SiO2
low quartz – kremeň
trigonal crystal
vitreous silica – kremenné sklo
amorphous
thermal expansion
coefficient (10-6 K-1)
α1 = 13
α3 = 8
α = 0.5
(isotropic)

## Slide 7
Descriptors (štruktúrne charakteristiky)
conceptual scheme that provides a precise quantitative characterization
of some aspect of structure
Examples:
bond length – dĺžka väzby
unit cell – elementárna (základná) bunka
symmetry elements – prvky symetrie
coordination number – koordinačné číslo
vacancy concentration – koncentrácia vakancií
grain size – veľkosť zŕn
correlation distance – korelačná vzdialenosť (dĺžka)

## Slide 8
Chemical bond – chemická väzba
bond type bond energy
bond length – dĺžka väzby 0.1 – 0.25 nm
covalent ~ 5 eV (8×10-19 J)
ionic 1 – 3 eV
metallic ~ 0.5 eV
van der Waals 0.001 – 0.1 eV
orbital hybridisation – sp2, sp3
sizes of atoms /ions – atomic radii – atómové polomery
depends on bond type
bond angles – uhol medzi väzbami (for covalent bonds)
sp2 – 120°
sp3 – 109.5°

## Slide 9
group of atoms
coordination number – koordinačné číslo
coordination shells – koordinačné sféry

## Slide 10
group of atoms
packing fraction – miera zaplnenia
Vi – volume of individual structural
units (atoms, molecules...)
VT – volume (macroscopic) of the sample
gases – Vv ~ 10-4
liquids and amorphous solids – Vv ~ 0.5

## Slide 11
Classification of materials
non-crystalline state
(amorphous)
crystalline state
liquid crystals
quasicrystals
statistical parameters
lack of tranlational symmetry!!
short range order – SRO
usporiadanosť nablízko
tranlational symmetry!!
long range order – LRO
usporiadanosť na diaľku
sharp diffraction spots in TEM
absence of translational symmetry or LRO
orientational order

## Slide 12
Non-crystalline state
liquid state – low viscosity kT > binding energy
glassy state – high viscosity kT < binding energy
similar structure – difference in dynamics
temperature
volume
crystal
glass
liquid
glass transition
melting
Tg
Tm
VF
VF
VF – free volume

## Slide 13
Pair distribution function
hard sphere model
r
g(r)
1
2R0
gas
4R0
r
g(r)
1
2R0
4R0
liquid/glass
r
g(r)
2R0
4R0
6
6
12
8
primitive cubic
monoatomic crystal
correlation
distance

## Slide 14
Hard sphere model – model tvrdých gúľ
average number of nearest neighbors
r
g(r)
Bernal – 1959 – Random close-packed sphere model
packing fraction Vv ~ 0.64
for fcc and hcp
NN = 12
Vv = 0.7405

## Slide 15
Random walk models – modely náhodnej prechádzky
applications:
shapes of flexible polymer molecules
Brownian motion
diffusion
1, 2, 3 dimensions
constant or variable step length
motion on fixed lattice
motion in any direction

## Slide 16
Random walk models – modely náhodnej prechádzky
step length – l
number of steps – n
end-to-end
displacement – Rn
uncorrelated motion
polymer chain
n spheres of diameter D0
packing fraction
root-mean-square displacement

## Slide 17
expanding – dilatation symmetry
Fractal models
fractal dimension D
fractal object with
“mass” M
size R
M ~ RD
D is an integer for compact objects

## Slide 18
Examples
Menger sponge
Koch snowflake
polymer chain

## Slide 19
Fractals in material science
Diffusion-limited aggregation
simulation of growth
Self-regulating heaters
polyethylene-carbon black composite
particles form conductive
fractal structures
Fracture
correlation between
fracture toughness
and
the fractal dimension
of the fracture surface