## Slide 1
Diffraction
Literature:
V. Valvoda, M. Polcarová, P. Lukáč: Základy strukturní analýzy,
Karolinum, Praha 1992
M. Birkholz: Thin Film Analysis by X-Ray Scattering, Wiley-WCH,
Weinheim 2006
properties of X-rays, high-energy electrons
and neutrons used in diffraction analysis
geometrical principles of diffraction
    Diffracted intensity – kinematical & dynamical theory
    Basic experimental techniques
    X-ray diffractometry
    Bragg-Brentano geometry
    Grazing incidence diffraction
    Crystallite size
    High resolution set-up
    X-ray topography

## Slide 2
Properties of X-rays, electrons and neutrons
X-rays electrons neutrons
charge 0 -e 0
rest mass 0 9.1×10-31 kg 1.67×10-27 kg
energy ~ 10 keV ~ 100 keV ~ 0.03 eV
wave length 0.15 nm 0.004 nm 0.12 nm
Bragg angles large ~ 1° large
extinction length ~ 10 μm 0.03 μm 100 μm
absorption length 100 μm 1 μm 5 cm

## Slide 3
Properties of X-rays, electrons and neutrons
X-rays electrons neutrons
rocking curve width 5” 0.6° 0.5”
refractive index n < 1 n > 1 n ≷ 1
atomic scatt. factors f 10-4 nm 1 nm 10-5 nm
dependence of f on Z ~ Z ~ Z2/3 irregular
anomalous dispersion common – rare
spectral width ~ 1 eV 3 eV 500 eV

## Slide 4: diffraction conditions – Laue equations
a, b, c
s0
s
Laue equations

## Slide 5: Concept of reciprocal lattice
scattering vector
reciprocal basis vectors
reciprocal lattice vectors

## Slide 6
Concept of reciprocal lattice
conditions for diffraction are fulfilled
properties of reciprocal lattice vectors

## Slide 7
Concept of reciprocal lattice
(120)

## Slide 8
Looking for solution
X-ray tube
1/λ
s0/λ
s/λ

## Slide 9
Ewald construction
1/λ
X-ray tube
sample
Ewald sphere
s0/λ
s/λ
origin of RL
Ewald construction is a graphical presentation
of the solution of Laue equations
reciprocal
lattice
polycrystalline
samples

## Slide 10: Lattice planes in two-dimensional lattice
dhkl
dhkl
dhkl
dhkl

## Slide 11: Bragg’s law
dhkl
θ
d sinθ
diffraction
triangle
Miller indices (hkl)
diffraction indices hkl
(110)
110, 220, 440

## Slide 12: Extinction length ξ
Dimension of coherent region << ξ kinematical theory
Dimension of coherent region ≥ ξ dynamical theory
D
Extremely important parameter
I0
I
I ≈ I0 ??
depends on
hkl, λ,
material

## Slide 13
Diffracted intensity
Kinematical theory of diffraction – 1st Born approximation
hierarchy of scattering – calculation of amplitude
electron – scattering length be (scattering amplitude) [m] ~ classical radius of electron (Thomson)
re = 2.82×10-6 nm
intensity of unpolarized radiation scattered by one free electron

## Slide 14
Diffracted intensity
atom – atomic form factor f – integration over the volume of atom
Cromer-Mann coefficients ai, bi, c– tabulated
f ’, f ” corrections for anomalous dispersion
for electrons
absolute units
electron units
electrons
X-rays
neutrons

## Slide 15
Diffracted intensity
unit cell – structure factor F(S) – summation over all atoms in cell
Debye-Waller factor
extinction rules  type of lattice, symmetry elements
xj, yj, zj –
fractional coordinates
– mean squared
displacement
Bj – temperature factors
tabulated

## Slide 16
Structure factor – example
Cu3Au – alloy
disordered form – fcc
ordered form –
primitive cubic
Cu
Au
random occupation
75% Cu
25% Au
quenching from 600°
annealing 20 days at 365°
and 40 days at 280°

## Slide 17
Diffracted intensity
whole lattice – summation over all unit cells
 interference function for intensity
lattice factor
intensity scattered by the whole crystal – interference function
fundamental equation
electron density
complex number –
phase factor!

## Slide 18
Angular dependence of intensity
Interference function
[atomic factor f(S)]2
intensity
S ~ sinθ/λ

## Slide 19
YBCO/sapphire
001
002
003

## Slide 20
Measured intensity
maximum intensity
area of the peak
for small single crystalline sample
phkl = 1
for polycrystalline sample
phkl = multiplicity factor
Lp – Lorentz-polarization factor
for small single
crystalline sample
for polycrystalline
sample
V – irradiated volume
quantitative analysis!
Integral intensity

## Slide 21
Parameters of diffraction peaks
FWHM or integral breadth βh is affected by
instrumental broadening – g(2θ)
crystallite size – β ~ λ/(D cosθ)
(Scherrer equation)
microstrain – β ~ tanθ
planar lattice defects
(stacking faults, antiphase boundaries)
convolution of line profiles
Gaussian
Cauchy – Lorentz

## Slide 22
Dynamical theory of diffraction
Intensity I ~ |F(S)|
Solution of wave equation in periodic medium (dielectric susceptibility)
for (nearly) ideal large single crystals
refraction od X-rays – n = 1 – δ δ ~ 10-5 ÷10-6
multiple diffraction – interaction of diffracted and primary beam

## Slide 23
Rocking curve – perfect crystal, Bragg case
Darwin curve
Prins curve
typical values of W:
Si 004, Cu Kα1 3.83 "
Si 333, Mo Kα1 0.73 "
GaAs 004, Cu Kα1 8.55 "

## Slide 24
Debye-Scherrer method
measuring of lattice parameters of powder samples with high precision

## Slide 25
Laue method
orientation of single crystals
Laue – 1912
FMFI UK – 1992

## Slide 26
X-Ray diffractometry
X-ray sources
sealed tubes ~ 1.5 kW
rotating anodes ~ 18 kW
synchrotron by orders of magnitude higher
goniometer
measuring the angles with precision ~ 0.0001°
PC controll
detectors
point – 0D
linear – 1D
area – 2D (films)

## Slide 27
Absorption of X-rays
Lambert-Beer law
μ – attenuation coefficient
I0
I
t
β filter

## Slide 28
incident
beam
diffracted
beam
sample
θ
θ
2θ
sample
surface
Symmetric θ/2θ (2θ/θ) measurement
2 configurations of diffractometers – horizontal or vertical set-up
fixed sample, moving X-ray tube and detector (θ-θ)
fixed tube, moving sample (θ) and detector (2θ), ratio of speeds – 1:2

## Slide 29: Diffraction in symmetric set-up
primary beam
Diffracting planes – parallel to the sample sufrace
Each diffraction originates from different assembly of crystallites

## Slide 30: Bragg-Brentano set-up
detector
focus of
X-ray tube
focussing
circle
sample
goniometer axis
Divergent primary beam irradiates the sample. All beams diffracted at different
parts of the sample are focused at the detector slit.
detector slit

## Slide 31: Diffraction pattern of MgB2 wire in Ti sheath
MgB2 and MgO phases are identified. Some peaks of Ti are also present. Red line is the simulated curve provided by software TOPAS 3.0 of Bruker company.