## Slide 1
Crystalline state
Symmetry in nature
Symmetry in arts and industry
Description of symmetry – basic concepts
Crystallography of two dimensions
Crystallography of three dimensions

## Slide 2
Symbols and conventions
one specific plane
all equivalent planes
one specific direction
all equivalent directions
multiplicity n – important parameter
Hexagonal or trigonal lattice systems – Bravais-Miller indices
a1
a2
a3
minus sign

## Slide 3
Transformation of indices
in some cases the use of new set of basis vectors is necessary
transition from the basis a1, a2, a3
to an other one A1, A2, A3
the same transformation matrix has to be used for indices
(HKL) are the Miller indices related to A1, A2, A3 and
(hkl) are the indices connected with a1, a2, a3

## Slide 4
Transformation of indices
a1
a2
a3
transition from Miller indices to Bravais-Miller indices
not trivial for directions
a1
a2

## Slide 5
Two-dimensional lattices

## Slide 6
Two-dimensional lattices
crystal system – oblique
sústava rovnobežníková,
klinogonálna
cell type – primitive
lattice parameters:
a ≠ b, γ ≠ 90°, 120°
a
b
γ

## Slide 7
Two-dimensional lattices
crystal system – orthogonal
sústava pravouhlá
cell type – primitive
lattice parameters:
a ≠ b, γ = 90°
a
b
γ

## Slide 8
Two-dimensional lattices
a
b
γ
crystal system – orthogonal
sústava pravouhlá
cell type – centered
lattice parameters:
a ≠ b, γ = 90°

## Slide 9
Two-dimensional lattices
crystal system – orthogonal
sústava pravouhlá
cell type – centered
lattice parameters:
a ≠ b, γ = 90°
a
b
γ

## Slide 10
Two-dimensional lattices
crystal system – tetragonal
sústava štvorcová
cell type – primitive
lattice parameters:
a = b, γ = 90°
a
b = a
γ

## Slide 11
Two-dimensional lattices
crystal system – hexagonal
sústava šesťuholníková
cell type – primitive
lattice parameters:
a = b, γ = 120°
a
b = a
γ

## Slide 12
Combination of point symmetry elements
crystal structures have more symmetry elements, which combinations are allowed?
2
m
possible combinations of two-fold axis with mirror line crossing the axis
m
2
2mm
NOT

## Slide 13
Matrix representation of symmetry operations
x
y
reflection
m ≡ x
x
y
reflection
m ≡ y
x
y
φ
rotation
axis at
origin
reflection through
arbitrarily
oriented line
x
y
φ

## Slide 14
Definition of group
A group is a set, G, together with an operation • (called the group law of G)
that combines any two elements a and b to form another element, denoted
a • b or ab. To qualify as a group, the set and operation, (G, •), must satisfy
four requirements known as the group axioms:
Inverse element
For each a in G, there exists an element b in G, commonly denoted a−1,
such that a • b = b • a = E, where E is the identity element.
Identity element
There exists an element E in G such that, for every element a in G,
the equation E • a = a • E = a holds. Such an element is unique,
and thus one speaks of the identity element.
Associativity
For all a, b and c in G, (a • b) • c = a • (b • c).
Closure
For all a, b in G, the result of the operation, a • b, is also in G.

## Slide 15
Symmetry groups – example
 | m1 | m2 | m3 | A1 | A2
m1 | E | A1 | A2 | m2 | m3
m2 | A2 | E | A1 | m3 | m1
m3 | A1 | A2 | E | m1 | m2
A1 | m3 | m1 | m2 | A2 | E
A2 | m2 | m3 | m1 | E | A1
m1
m3
m2
three mirror lines m1, m2, m3
two rotations
counter-clockwise A1(120°),
clockwise A2(-120°)
three-fold axis in
the center
group multiplication table

## Slide 16
Group and subgroup – podgrupa
 | m1 | m2 | m3 | A1 | A2
m1 | E | A1 | A2 | m2 | m3
m2 | A2 | E | A1 | m3 | m1
m3 | A1 | A2 | E | m1 | m2
A1 | m3 | m1 | m2 | A2 | E
A2 | m2 | m3 | m1 | E | A1
m1
m3
m2
(A1, A2, E) is a subgroup of (m1, m2, m3, A1, A2, E)

## Slide 17
Point groups and space groups
– bodové grupy a priestorové grupy
Point groups contain only point symmetry operations (reflections, rotations,
etc.), no operations with translations
Space groups contain symmetry operations involving translational components
– either perfect or partial
Generally –
Point groups are NOT a subgroups of the corresponding space group
for each structure the knowledge of both groups is important
Macroscopic physical properties are determined
by the point group of the crystal structure
The knowledge of complete space group is necessary
for the precise description of the structure on microscopic level

## Slide 18
Point groups in 2D
Can be created by combination of rotation axes
and the intersecting mirror lines
Theorem 1: Combination of a rotation axis Aα and an intersecting mirror line m1
implies the existence of a second mirror line m2 which also passes through Aα
and makes an angle α/2 with m1.
Aα
m1
m2
Aα/2
This is the answer, why

## Slide 19
Ten point groups in 2D
International notation (Hermann-Mauguin) – Schönflies notation
1 C1
2 C2
3 C3
4 C4
6 C6
m Cs
2mm C2v
3m C3v
4mm C4v
6mm C6v

## Slide 20
Combination of rotation axes with translations
Theorem 2: A rotation about an axis A through an angle α, followed by a translation T perpendicular to the axis, is equivalent to a rotation through the same angle α, in the same sense, but about an axis B situated on the perpendicular bisector of AA’ and at a distance from AA’.
A’α
Aα
α
Bα
d
T

## Slide 21
Position of axes in unit cells
Oblique crystal system

## Slide 22
Position of axes in unit cells
Orthogonal crystal system
primitive cell

## Slide 23
Position of axes in unit cells
Orthogonal crystal system
centered cell

## Slide 24
Position of axes in unit cells
Tetragonal crystal system

## Slide 25
Position of axes in unit cells
Hexagonal crystal system

## Slide 26
Combination of mirror lines with translations
translation T perpendicular to mirror line m
m
m
T
m’

## Slide 27
Combination of mirror lines with translations
translation T not perpendicular to mirror line m
m
m
T
T‖
g

## Slide 28
17 space groups for two dimensions (wallpaper groups)
– plane groups – rovinné (priestorové) grupy
number | system | cell | point group | plane group
1 | oblique | primitive | 1 | p1
2 |  | primitive | 2 | p211
3 | orthogonal | primitive | m | p1m1
4 |  | primitive |  | p1g1
5 |  | centered |  | c1m1
6 |  | primitive | 2mm | p2mm
7 |  | primitive |  | p2mg
8 |  | primitive |  | p2gg
9 |  | centered |  | c2mm
10 | tetragonal | primitive | 4 | p4
11 |  | primitive | 4mm | p4mm
12 |  | primitive |  | p4gm
13 | hexagonal | primitive | 3 | p3
14 |  | primitive | 3m | p3m1
15 |  | primitive |  | p31m
16 |  | primitive | 6 | p6
17 |  | primitive | 6mm | p6mm